# Supporting Information

### Low temperature enantiotropic nematic phases from V-shaped, shape-persistent molecules

### Matthias Lehmann* and Jens Seltmann

### Address: Institute of Chemistry, Chemnitz University of Technology, Straße der Nationen 62, 09111 Chemnitz, Germany

### Email: Matthias Lehmann - Matthias.Lehmann@chemie.tu-chemnitz.de

### *Corresponding author

General procedure for preparation of iodobenzenes 5a–e

In a nitrogen atmosphere a mixture of 1.0 equiv of 4-iodophenol, 1.3 equiv of K2CO3 in dried DMF was heated to 55 °C. Thereto 1.0 equiv of ethyl ω-bromoalkanoate was added and the mixture was stirred over night at this temperature. Water and ethyl acetate were added and the product was extracted into the organic solvent. The organic solution was washed with saturated brine and dried with anhydrous sodium sulphate. The extract was filtered and concentrated in vacuo.

Ethyl 5-(4-iodophenoxy)pentanoate (5a) bright purple oil; yield 2.9 g (92%). 1H NMR (400 MHz, CDCl3): ( = 7.53 (2H, AA’BB’), 6.65 (2H, AA’BB’), 4.12 (q, 2H, COOCH2CH3, J = 7.2), 3.92 (m, 2H, OCH2), 2.36 (m, 2H, CH2–COOEt), 1.80 (m, 4H, CH2), 1.25 (t, 3H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.3 (Cq, C=O), 158.7 (Cq, C–OCH2), 138.1 (Ct), 116.8 (Ct), 82.6 (Cq, C–I), 67.4 (OCH2), 60.3 (COOCH2CH3), 33.8 (CH2COOEt), 28.5, 21.5 (CH2), 14.3 (CH3).

Ethyl 6-(4-iodophenoxy)hexanoate (5b) bright purple oil; yield 2.9 g (92%). NMR data are identical to whose reported in literature [1].

Ethyl 7-(4-iodophenoxy)heptanoate (5c) bright orange oil; yield 2.9 g (84%). 1H NMR (400 MHz, CDCl3): ( = 7.51 (2H, AA’BB’), 6.64 (2H, AA’BB’), 4.11 (q, 2H, OCH2CH3, J = 7.2), 3.88 (t, 2H, OCH2, J = 6.8), 2.29 (t, 2H, CH2COOEt, J = 7.4), 1.75 (m, 2H, CH2), 1.64 (m, 2H, CH2), 1.47–1.35 (m, 4H, CH2), 1.24 (t, 3H, CH3, J = 7.1); 13C NMR (100 MHz, CDCl3): δ = 173.8 (Cq, C=O), 159.0 (Cq, C–OCH2), 138.2 (Ct), 116.9 (Ct), 82.5 (Cq, C–I), 67.9 (OCH2), 60.3 (COOCH2CH3), 34.3 (CH2COOEt), 29.0, 28.9, 25.7, 24.9 (CH2), 14.3 (CH3).

Ethyl 8-(4-iodophenoxy)octanoate (5d) bright purple oil; yield 2.3 g (86%). 1H NMR (400 MHz, CDCl3): ( = 7.51 (2H, AA’BB’), 6.63 (2H, AA’BB’), 4.10 (q, 2H, OCH2CH3, J = 7.2), 3.87 (t, 2H, OCH2, J = 6.4), 2.28 (t, 2H, CH2COOEt, J = 7.2), 1.73 (m, 2H, CH2), 1.61 (m, 2H, CH2), 1.47–1.32 (m, 6H, CH2), 1.24 (t, 3H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.9 (Cq, C=O), 159.0 (Cq, C–OCH2), 138.2 (Ct), 116.9 (Ct), 82.5 (Cq, C–I), 67.9 (OCH2), 60.3 (COOCH2CH3), 34.3 (CH2COOEt), 29.1, 29.0, 25.8, 24.9 (CH2), 14.3 (CH3).

Ethyl 11-(4-iodophenoxy)undecanoate (5e) fawn solid; yield 2.6 g (88%). 1H NMR (400 MHz, CDCl3): ( = 7.52 (2H, AA’BB’), 6.65 (2H, AA’BB’), 4.12 (q, 2H, OCH2CH3, J = 7.2), 3.90 (t, 2H, OCH2, J = 6.4), 2.28 (t, 2H, CH2COOEt, J = 7.2), 1.75 (m, 2H, CH2), 1.61 (m, 2H, CH2), 1.45–1.26 (m, 10H, CH2), 1.25 (t, 3H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.1 (Cq, C=O), 159.1 (Cq, C–OCH2), 138.2 (Ct), 117.0 (Ct), 82.5 (Cq, C–I), 68.2 (OCH2), 60.3 (COOCH2CH3), 34.5 (CH2COOEt), 29.6, 29.48, 29.44, 29.36, 29.2, 26.1, 25.1 (CH2), 14.4 (CH3).

General procedure for preparation of terminal alkynes 6a–e

A mixture of 1.0 equiv of alkyne 4, 1.0 equiv of the corresponding iodophenol derivative 5a–e, 0.1 equiv of Pd(PPh3)4 and 0.05 equiv of CuI in 50 ml piperidine is stirred for 1 h at room temperature. Afterwards the solvent is removed in vacuo and the intermediate products are isolated by column chromatography using a mixture of EtOAc/hexane. These products are treated with 1.5 equiv of TBAF in 40 ml THF and are stirred for 1 h at room temperature. After removing the solvent in vacuo the terminal alkynes 6a–e are purified by column chromatography with a mixture of EtOAc/hexane.

Ethyl 5-[4-({2,5-bis(hexyloxy)-4-(ethynyl)phenyl}ethynyl)phenoxy]pentanoate (6a) Hexane/EtOAc = 5/1 (Rf = 0.45), bright yellow solid; yield 0.38 g (80%). 1H NMR (400 MHz, CDCl3): ( = 7.45 (2H, AA’BB’), 6.97 (s, 1H), 6.96 (s, 1H), 6.85 (2H, AA’BB’), 4.11 (q, 2H, COOCH2CH3, J = 7.2), 3.98 (m, 6H, OCH2), 3.33 (s, 1H, C(CH), 2.34 (m, 2H, CH2COOEt), 1.83 (m, 8H, CH2), 1.52 (m, 4H, CH2), 1.35 (m, 8H, CH2), 1.22 (t, 3H, CH3, J = 6.8), 0.90 (m, 6H, CH3); 13C NMR (100 MHz, CDCl3): δ = 173.6 (Cq, C=O), 158.1 (Cq, C–OCH2), 154.3, 153.4 (Cq, C–OC6H13), 133.3 (Ct), 117.9, 116.8 (Ct), 115.5, 115.2 (Cq), 114.6 (Ct), 112.1 (Cq), 95.2, 84.5, 82.2, 80.2 (C(C), 69.8, 69.7, 67.6 (OCH2), 60.5 (COOCH2CH3), 34.1 (CH2COOEt), 31.74, 31.67, 29.4, 29.2, 28.7, 25.9, 25.7, 22.8, 22.7, 21.8 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C35H46O5: C 76.89, H 8.48; Found: C 76.82, H 8.50; FD MS: m/z [%]: 548.4 (7, [M+2]+); 547.4 (41, [M+1]+); 546.4 (100, M+).

Ethyl 6-[4-({2,5-bis(hexyloxy)-4-(ethynyl)phenyl}ethynyl)phenoxy]hexanoate (6b) Hexane/EtOAc = 5/1 (Rf = 0.4), bright yellow solid; yield 0.5 g (58%). 1H NMR (400 MHz, CDCl3): ( = 7.45 (2H, AA’BB’), 6.97 (s, 1H), 6.96 (s, 1H), 6.85 (2H, AA’BB’), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 3.98 (m, 6H, OCH2), 3.33 (s, 1H, C(CH), 2.34 (t, 2H, CH2COOEt, J = 7.2), 1.81 (m, 8H, CH2), 1.71 (m, 2H, CH2), 1.52 (m, 4H, CH2), 1.34 (m, 8H, CH2), 1.26 (t, 3H, CH3, J = 7.2), 0.90 (m, 6H, CH3); 13C NMR (100 MHz, CDCl3): δ = 173.8 (Cq, C=O), 159.3 (Cq, C–OCH2), 154.3, 153.3 (Cq, C–OC6H13), 133.3 (Ct), 117.9, 116.8 (Ct), 115.4, 115.2 (Cq), 114.5 (Ct), 112.1 (Cq), 95.2, 84.4, 82.2, 80.2 (C(C), 69.71, 69.67, 67.8 (OCH2), 60.4 (COOCH2CH3), 34.3 (CH2COOEt), 31.7, 31.6, 29.2, 29.2, 29.0, 25.8, 25.7, 24.8, 22.74, 22.69 (CH2), 14.3, 14.2, 14.1 (CH3); EA: Calc. for C36H48O5: C 77.11, H 8.63; Found: C 76.87, H 8.76; FD MS: m/z [%]: 559.9 (100, M+).

Ethyl 7-[4-({2,5-bis(hexyloxy)-4-(ethynyl)phenyl}ethynyl)phenoxy]heptanoate (6c) Hexane/EtOAc = 10/1 (Rf = 0.4), bright yellow solid; yield 0.75 g (70%). 1H NMR (400 MHz, CDCl3): ( = 7.45 (2H, AA’BB’), 6.97 (s, 1H), 6.96 (s, 1H), 6.85 (2H, AA’BB’), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 3.98 (m, 6H, OCH2), 3.33 (s, 1H, C(CH), 2.31 (t, 2H, CH2COOEt, J = 7.2), 1.81 (m, 6H, CH2), 1.66 (m, 2H, CH2), 1.53–1.32 (m, 16H, CH2), 1.25 (t, 3H, CH3, J = 7.2), 0.90 (m, 6H, CH3); 13C NMR (100 MHz, CDCl3): ( = 173.9 (Cq, C=O), 159.4 (Cq, C–OCH2), 154.3, 153.4 (Cq, C–OC6H13), 133.2 (Ct), 117.9, 116.8 (Ct), 115.4, 115.2 (Cq), 114.6 (Ct), 112.1 (Cq), 95.3, 84.4, 82.2, 80.2 (C(C), 69.75, 67.70 (OCH2), 60.4 (COOCH2CH3), 34.4 (CH2COOEt), 31.7, 31.6, 29.4, 29.2, 29.1, 29.0, 25.8, 25.7, 24.9, 22.8, 22.7 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C37H50O5: C 77.31, H 8.77; Found: C 77.09, H 8.88; FD MS: m/z [%]: 574.0 (100, M+).

Ethyl 8-[4-({2,5-bis(hexyloxy)-4-(ethynyl)phenyl}ethynyl)phenoxy]octanoate (6d) Hexane/EtOAc = 15/1 (Rf = 0.25), colourless solid; yield 0.64 g (90%). 1H NMR (400 MHz, CDCl3): ( = 7.45 (2H, AA’BB’), 6.97 (s, 1H), 6.96 (s, 1H), 6.85 (2H, AA’BB’), 4.11 (q, 2H, COOCH2CH3, J = 7.2), 3.98 (m, 6H, OCH2), 3.33 (s, 1H, C≡CH), 2.30 (t, 2H, CH2–COOEt, J = 7.2), 1.80 (m, 6H, CH2), 1.64 (m, 2H, CH2), 1.48 (m, 6H, CH2), 1.35 (m, 12H, CH2), 1.25 (t, 3H, CH3, J = 7.2), 0.90 (m, 6H, CH3); 13C NMR (100 MHz, CDCl3): δ = 174.0 (Cq, C=O), 159.4 (Cq, C–OCH2), 154.3, 153.3 (Cq, C–OC6H13), 133.2 (Ct), 117.9, 116.8 (Ct), 115.3, 115.2 (Cq), 114.6 (Ct), 112.1 (Cq), 95.3, 84.4, 82.2, 80.2 (C≡C), 69.8, 69.7, 68.1 (OCH2), 60.3 (COOCH2CH3), 34.5 (CH2COOEt), 31.74, 31.67, 29.4, 29.2, 29.17, 29.15, 26.0, 25.9, 25.7, 25.0, 22.8, 22.7 (CH2), 14.4, 14.20, 14.18 (CH3); FD MS: m/z [%]: 588.8 (45, [M+1]+); 587.8 (100, M+).

Ethyl 11-[4-({2,5-Bis(hexyloxy)-4-(ethynyl)phenyl}ethynyl)phenoxy]undecanoate (6e) Hexane/EtOAc = 15/1 (Rf = 0.25), colourless solid; yield 1.2 g (87%). 1H NMR (400 MHz, CDCl3): δ = 7.45 (2H, AA’BB’), 6.97 (s, 1H), 6.96 (s, 1H), 6.85 (2H, AA’BB’), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 3.98 (m, 6H, OCH2), 3.33 (s, 1H, C≡CH), 2.28 (t, 2H, CH2–COOEt, J = 7.2), 1.86–1.72 (m, 6H, CH2), 1.61 (m, 2H, CH2), 1.56–1.40 (m, 6H, CH2), 1.39–1.26 (m, 18H, CH2), 1.25 (t, 3H, CH3, J = 7.2), 0.89 (m, 6H, CH3); 13C NMR (100 MHz, CDCl3): δ = 174.0 (Cq, C=O), 159.4 (Cq, C–OCH2), 154.3, 153.3 (Cq, C–OC6H13), 133.1 (Ct), 117.9, 116.7 (Ct), 115.3, 115.2 (Cq), 114.6 (Ct), 112.1 (Cq), 95.3, 84.4, 82.2, 80.2 (C(C), 69.72, 69.67, 68.1 (OCH2), 60.3 (COOCH2CH3), 34.5 (CH2COOEt), 31.73, 31.65, 29.6, 29.48, 29.47, 29.41, 29.36, 29.30, 29.24, 26.1, 25.8, 25.7, 25.1, 22.8, 22.7 (CH2), 14.4, 14.17, 14.16 (CH3).

Analytical data of hockey stick compounds 3b–e.

2-{4-[4-{4-[(5-Ethoxycarbonyl)pentyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-(4-bromophenyl)-1,3,4-thiadiazole (3b) Hexane/EtOAc = 6/1 (Rf = 0.25), yellow solid; yield 0.15 g (57%). 1H NMR (400 MHz, CDCl3): ( = 7.99 (2H, AA’BB’), 7.88 (2H, AA’BB’), 7.64 (4H, AA’BB’), 7.45 (2H, AA’BB’), 7.02 (s, 1H), 7.01 (s, 1H), 6.85 (2H, AA’BB’), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 4.04 (t, 2H, OCH2, J = 6.4), 4.03 (t, 2H, OCH2, J = 6.4), 3.98 (t, 2H, OCH2, J = 6.4), 2.34 (t, 2H, CH2COOEt, J = 7.2), 1.84 (m, 6H, CH2), 1.71 (m, 2H, CH2), 1.52 (m, 4H, CH2), 1.36 (m, 8H, CH2), 1.26 (t, 3H, CH3, J = 7.2), 0.91 (t, 3H, CH3, J = 7.2), 0.90 (t, 3H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.8 (Cq, C=O), 167.9, 167.2 (Cq, N=C–S), 159.3 (Cq, C–OCH2), 154.0, 153.3 (Cq, C–OC6H13), 133.2, 132.6, 132.4 (Ct), 129.4 (Ct), 129.1 (Cq), 127.9 (Ct), 126.8, 125.8 (Cq), 117.0, 116.8 (Ct), 115.4, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.0, 89.2, 84.7 (C(C), 69.8, 69.7, 67.8 (OCH2), 60.4 (COOCH2CH3), 34.4 (CH2COOEt), 31.7, 29.5, 29.4, 29.0, 25.9, 25.8, 24.8, 22.8 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C50H55BrN2O5S: C 68.56, H 6.33, N 3.20, S 3.66; Found: C 68.13, H 6.09, N 3.24, S 3.55; FD MS: m/z [%]: 875.7 (100, [M+2]+); 873.7 (77, M+).

2-{4-[4-{4-[6-(Ethoxycarbonyl)hexyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-(4-bromophenyl)-1,3,4-thiadiazole (3c) Hexane/EtOAc = 6/1 (Rf = 0.35), yellow solid; yield 0.33 g (66%). 1H NMR (400 MHz, CDCl3): ( = 7.99 (2H, AA’BB’), 7.88 (2H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (2H, AA’BB’), 7.02 (s, 1H), 7.01 (s, 1H), 6.86 (2H, AA’BB’), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 4.04 (t, 2H, OCH2, J = 6.4), 4.03 (t, 2H, OCH2, J = 6.4), 3.97 (t, 2H, OCH2, J = 6.4), 2.32 (t, 2H, CH2COOEt, J = 7.2), 1.84 (m, 6H, CH2), 1.67 (m, 2H, CH2), 1.59–1.35 (m, 16H, CH2), 1.26 (t, 3H, CH3, 3JHH = 7.2), 0.91 (t, 3H, CH3, J = 7.2), 0.90 (t, 3H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.9 (Cq, C=O), 167.9, 167.2 (Cq, N=C–S), 159.4 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.6, 132.4 (Ct), 129.4 (Ct), 129.1 (Cq), 127.9 (Ct), 126.8, 125.8 (Cq), 117.0, 116.8 (Ct), 115.4, 115.2 (Cq), 114.6 (Ct), 112.8 (Cq), 95.6, 94.0, 89.2, 84.7 (C(C), 69.8, 69.7, 68.0 (OCH2), 60.4 (COOCH2CH3), 34.4 (CH2COOEt), 31.8, 29.5, 29.4, 29.1, 29.0, 25.90, 25.88, 25.0, 22.82, 22.80 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C51H57BrN2O5S: C 68.83, H 6.46, N 3.15, S 3.60; Found: C 68.31, H 6.19, N 3.22, S 3.50; FD MS: m/z [%]: 889.8 (100, [M+2]+); 887.9 (40, M+).

2-{4-[4-{4-[7-(Ethoxycarbonyl)heptyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-(4-bromophenyl)-1,3,4-thiadiazole (3d) Hexane/EtOAc = 6/1 (Rf = 0.35), yellow solid; yield 0.32 g (51%). 1H NMR (400 MHz, CDCl3): ( = 7.99 (2H, AA’BB’), 7.88 (2H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (2H, AA’BB’), 7.02 (s, 1H), 7.01 (s, 1H), 6.86 (2H, AA’BB’), 4.10 (q, 2H, COOCH2CH3, J = 7.2), 4.03 (t, 2H, OCH2, J = 6.4), 4.02 (t, 2H, OCH2, J = 6.4), 3.97 (t, 2H, OCH2, J = 6.4), 2.30 (t, 2H, CH2COOEt, J = 7.2), 1.90–1.75 (m, 6H, CH2), 1.64 (m, 2H, CH2), 1.60–1.44 (m, 12H, CH2), 1.36 (m, 12H, CH2), 1.26 (t, 3H, CH3, 3JHH = 7.2), 0.91 (t, 3H, CH3, 3JHH = 7.2), 0.90 (t, 3H, CH3, 3JHH = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.0 (Cq, C=O), 167.9, 167.2 (Cq, N=C–S), 159.4 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.6, 132.2 (Ct), 129.4 (Ct), 129.1 (Cq), 127.9 (Ct), 126.8, 125.8 (Cq), 117.0, 116.7 (Ct), 115.3, 115.2 (Cq), 114.6 (Ct), 112.8 (Cq), 95.6, 94.0, 89.2, 84.6 (C(C), 69.8, 69.7, 68.1 (OCH2), 60.4 (COOCH2CH3), 34.5 (CH2COOEt), 31.8, 29.5, 29.4, 29.3, 29.18, 29.16, 26.0, 25.9, 25.0, 22.81, 22.80 (CH2), 14.4, 14.2 (CH3); FD MS: m/z [%]:903.5 (100, [M+2]+); 901.5 (83, M+).

2-{4-[4-{4-[10-(Ethoxycarbonyl)decyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-(4-bromophenyl)-1,3,4-thiadiazole (3e) Hexane/EtOAc = 6/1 (Rf = 0.30), yellow solid; yield 0.46 g (58%). 1H NMR (400 MHz, CDCl3): ( = 8.00 (2H, AA’BB’), 7.89 (2H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (2H, AA’BB’), 7.02 (s, 1H), 7.01 (s, 1H), 6.87 (2H, AA’BB’), 4.12 (q, 2H, COOCH2CH3, J = 7.2), 4.044 (t, 2H, OCH2, J = 6.4), 4.036 (t, 2H, OCH2, J = 6.4), 3.97 (t, 2H, OCH2, J = 6.4), 2.29 (t, 2H, CH2COOEt, J = 7.2), 1.90–1.74 (m, 6H, CH2), 1.60–1.50 (m, 8H, CH2), 1.40–1.28 (m, 18H, CH2), 1.26 (t, 3H, CH3, 3JHH = 7.2), 0.91 (t, 3H, CH3, J = 7.2), 0.90 (t, 3H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.1 (Cq, C=O), 167.9, 167.2 (Cq, N=C–S), 159.5 (Cq, C–OCH2), 154.0, 153.6 (Cq, C–OC6H13), 133.2, 132.6, 132.3 (Ct), 129.4 (Ct), 129.2 (Cq), 127.9 (Ct), 126.8, 125.8 (Cq), 117.1, 116.9 (Ct), 115.4 (Cq), 114.7 (Ct), 112.9 (Cq), 95.7, 94.0, 89.3, 84.7 (C≡C), 69.9, 69.7, 68.2 (OCH2), 60.3 (COOCH2CH3), 34.5 (CH2COOEt), 31.8, 29.6, 29.5, 29.39, 29.35, 29.28, 26.2, 25.9, 25.1, 22.8 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C55H65BrN2O5S: C 69.82, H 6.92, N 2.96, S 3.39; Found: C 69.88, H 6.77, N 3.25, S 3.22; FD MS: m/z [%]: 946.2 (100, M+).

Analytical data of V-shaped mesogens 1b–e and 2a–g.

2,5-Bis{4-[4-{4-[5-(ethoxycarbonyl)pentyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (1b) Hexane/EtOAc = 6/1 (Rf = 0.1), yellow solid; yield 95 mg (54%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.13 (q, 4H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.98 (t, 4H, OCH2, J = 6.4), 2.34 (t, 4H, CH2COOEt, J = 7.2), 1.85 (m, 12H, CH2), 1.71 (m, 4H, CH2), 1.55 (m, 12H, CH2), 1.37 (m, 16H, CH2), 1.26 (t, 6H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.8 (Cq, C=O), 167.9 (Cq, N=C–S), 159.3 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.3 (Ct), 129.6 (Cq), 127.9 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.4, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.7 (C(C), 69.8, 69.7, 67.8 (OCH2), 60.4 (COOCH2CH3), 34.4 (CH2COOEt), 31.8, 29.46, 29.45, 29.0, 25.9, 25.8, 24.8, 22.81, 22.80 (CH2); 14.4, 14.2 (CH3); EA: Calc. for C86H102N2O10S: C 76.19, H 7.58, N 2.07, S 2.37; Found: C 76.21, H 7.40, N 2.17, S 2.31; FD MS: m/z [%]: 1355.7 (45, [M+2]+); 1354.7 (78, [M+1]+); 1353.7 (100, M+).

2,5-Bis{4-[4-{4-[6-(ethoxycarbonyl)hexyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (1c) Hexane/EtOAc = 7/1 (Rf = 0.1), yellow solid; yield 100 mg (68%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.13 (q, 4H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.97 (t, 4H, OCH2, J = 6.4), 2.32 (t, 4H, CH2COOEt, J = 7.2), 1.87–1.78 (m, 12H, CH2), 1.67 (m, 4H, CH2), 1.52 (m, 16H, CH2), 1.37 (m, 16H, CH2), 1.26 (t, 6H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.9 (Cq, C=O), 167.8 (Cq, N=C–S), 159.4 (Cq, C–OCH2), 154.0, 153.5, (Cq, C–OC6H13), 133.2, 132.3 (Ct), 129.6 (Cq), 127.9 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.4, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.7 (C(C), 69.8, 69.7, 68.0 (OCH2), 60.4 (COOCH2CH3), 34.4 (CH2COOEt), 31.8, 29.5, 29.4, 29.2, 29.0, 25.90, 25.88, 25.0, 22.82, 22.80 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C88H106N2O10S: C 76.38, H 7.72, N 2.02, S 2.32; Found: C 75.90, H 7.29, N 2.23, S 2.17; FD MS: m/z [%]: 1382.7 (93, [M+1]+); 1381.7 (100, M+).

2,5-Bis{4-[4-{4-[7-(ethoxycarbonyl)heptyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (1d) Hexane/EtOAc = 6/1 (Rf = 0.1), yellow solid; yield 75 mg (50%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.13 (q, 4H, COOCH2CH3, 3JHH = 7.2), 4.05 (t, 4H, OCH2, 3JHH = 6.4), 4.04 (t, 4H, OCH2, 3JHH = 6.4), 3.97 (t, 4H, OCH2, 3JHH = 6.4), 2.30 (t, 4H, CH2–COOEt, 3JHH = 7.2), 1.90–1.75 (m, 12H, CH2), 1.68–1.32 (m, 42H, CH2), 1.26 (t, 6H, CH3, 3JHH = 7.2), 0.91 (t, 6H, CH3, 3JHH = 7.2), 0.90 (t, 6H, CH3, 3JHH = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.0 (Cq, C=O), 167.8 (Cq, N=C–S), 159.4 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.4 (Ct), 129.6 (Cq), 128.0 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.4, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.6 (C(C), 69.8, 69.7, 68.1 (OCH2), 60.4 (COOCH2CH3), 34.5 (CH2COOEt), 31.8, 29.5, 29.4, 29.3, 29.2, 26.9, 25.9, 25.0, 22.82, 22.80 (CH2), 14.4, 14.2 (CH3); FD-MS: m/z [%]: 1410.5 (63, [M+1]+); 1409.5 (67, M+); 705.0 (100, M2+).

2,5-Bis{4-[4-{4-[10-(ethoxycarbonyl)decyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (1e) Hexane/EtOAc = 13/1 (Rf = 0.07), yellow solid; yield 80 mg (51%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.65 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.87 (4H, AA’BB’), 4.13 (q, 4H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.97 (t, 4H, OCH2, J = 6.4), 2.29 (t, 4H, CH2COOEt, J = 7.2), 1.90–1.75 (m, 12H, CH2), 1.66–1.51 (m, 16H, CH2), 1.50–1.30 (m, 36H, CH2), 1.26 (t, 6H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.1 (Cq, C=O), 167.8 (Cq, N=C–S), 159.5 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.4 (Ct), 129.6 (Cq), 128.0 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.3, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.6 (C(C), 69.8, 69.7, 68.2 (OCH2), 60.3 (COOCH2CH3), 34.5 (CH2COOEt), 31.8, 29.6, 29.52, 29.47, 29.45, 29.40, 29.34, 29.27, 26.1, 25.9, 25.1, 22.82, 22.80 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C96H122N2O10S: C 77.07, H 8.22, N 1.87, S 2.14; Found: C 76.54, H 7.76, N 2.13, S 2.22; FD MS: m/z [%]: 1494.6 (100, [M+1]+); 1493.6 (93, M+).

2-{4-[4-{4-[5-(Ethoxycarbonyl)pentyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-{4-[4-{4-[4-(ethoxycarbonyl)butoxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (2a) Hexane/EtOAc = 7/1 (Rf = 0.1), yellow solid; yield 87 mg (61%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.135 (q, 2H, COOCH2CH3, J = 7.2), 4.134 (q, 2H, COOCH2CH3, J = 7.2), 4.043 (t, 4H, OCH2, J = 6.4), 4.036 (t, 4H, OCH2, J = 6.4), 3.98 (m, 4H, OCH2), 2.39 (t, 2H, CH2COOEt, J = 7.2), 2.34 (t, 2H, CH2COOEt, J = 7.2), 1.85 (m, 12H, CH2), 1.71 (m, 2H, CH2), 1.55 (m, 12H, CH2), 1.37 (m, 16H, CH2), 1.262 (t, 3H, CH3, J = 7.2), 1.259 (t, 3H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.8, 173.6 (Cq, C=O), 167.9 (Cq, N=C–S), 159.3, 159.2 (Cq, C–OCH2), 154.0, 153.5, (Cq, C–OC6H13), 133.2, 132.3 (Ct), 129.6 (Cq), 127.9 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.5, 115.4, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.7 (C(C), 69.8, 69.7, 67.8, 67.6 (OCH2), 60.5, 60.4 (COOCH2CH3), 34.4, 34.1 (CH2COOEt), 31.8, 29.5, 29.0, 28.8, 25.9, 25.8, 24.8, 22.8, 21.7 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C85H100N2O10S: C 76.09, H 7.51, N 2.09, S 2.39; Found: C 76.49, H 7.51, N 2.16, S 2.30; FD MS: m/z [%]:1340.7 (88, [M+1]+); 1339.7 (100, M+).

2-{4-[4-{4-[6-(Ethoxycarbonyl)hexyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-{4-[4-{4-[4-(ethoxycarbonyl)butoxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (2b) Hexane/EtOAc = 7/1 (Rf = 0.1), yellow solid; yield 90 mg (60%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.14 (q, 2H, COOCH2CH3, J = 7.2), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.99 (m, 4H, OCH2), 2.40 (t, 2H, CH2COOEt, J = 7.2), 2.32 (t, 2H, CH2COOEt, J = 7.2), 1.85 (m, 14H, CH2), 1.67 (m, 2H, CH2), 1.52 (m, 12H, CH2), 1.37 (m, 16H, CH2), 1.264 (t, 3H, CH3, J = 7.2), 1.258 (t, 3H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.8, 173.6 (Cq, C=O), 167.9 (Cq, N=C–S), 159.3, 159.2 (Cq, C–OCH2), 154.0, 153.5, (Cq, C–OC6H13), 133.2, 132.3 (Ct), 129.6 (Cq), 127.9 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.5, 115.4, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.7 (C(C), 69.8, 69.7, 67.8, 67.6 (OCH2), 60.5, 60.4 (COOCH2CH3), 34.4, 34.1 (CH2COOEt), 31.8, 29.5, 29.0, 28.8, 25.9, 25.8, 24.8, 22.8, 21.7 (CH2), 14.4, 14.2 (CH3). EA: Calc. for C86H102N2O10S: C 76.19, H 7.58, N 2.07, S 2.37; Found: C 75.91, H 7.87, N 1.95, S 2.25. FD MS: m/z [%]:1355.3 (90, M+); 1354.3 (100).

2-{4-[4-{4-[7-(Ethoxycarbonyl)heptyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-{4-[4-{4-[4-(ethoxycarbonyl)butoxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (2c) Hexane/EtOAc = 7/1 (Rf = 0.1), yellow solid; yield 91 mg (63%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.14 (q, 2H, COOCH2CH3, J = 7.2), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.98 (m, 4H, OCH2), 2.39 (t, 2H, CH2COOEt, J = 7.2), 2.30 (t, 2H, CH2COOEt, J = 7.2), 1.90–1.76 (m, 14H, CH2), 1.68–1.51 (m, 10H, CH2), 1.50 – 1.32 (m, 22H, CH2), 1.264 (t, 3H, CH3, J = 7.2), 1.258 (t, 3H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.0, 173.6 (Cq, C=O), 167.8 (Cq, N=C–S), 159.4, 159.2 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.4 (Ct), 129.6 (Cq), 128.0 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.5, 115.4, 115.21, 115.18 (Cq), 114.62, 114.61 (Ct), 112.89, 112.87 (Cq), 95.6, 95.5, 94.1, 89.2, 84.7, 84.6 (C(C), 69.8, 69.7, 68.1, 67.6 (OCH2), 60.5, 60.4 (COOCH2CH3), 34.5, 34.1 (CH2COOEt), 31.8, 29.5, 29.3, 29.2, 28.7, 26.0, 25.9, 25.0, 22.82, 22.80, 21.8 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C87H104N2O10S: C 76.28, H 7.65, N 2.05, S 2.34; Found: C 75.81, H 7.37, N 2.23, S 2.23; FD MS: m/z [%]: 1368.6 (90, [M+1]+); 1367.6 (100, M+).

2-{4-[4-{4-[5-(Ethoxycarbonyl)pentyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-{4-[4-{4-[6-(ethoxycarbonyl)hexyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (2d) Hexane/EtOAc = 7/1 (Rf = 0.1), yellow solid; yield 95 mg (65%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.85 (4H, AA’BB’), 4.133 (q, 2H, COOCH2CH3, J = 7.2), 4.128 (q, 2H, COOCH2CH3, J = 7.2), 4.042 (t, 4H, OCH2, J = 6.4), 4.035 (t, 4H, OCH2, J = 6.4), 3.98 (t, 2H, OCH2, J = 6.4), 3.97 (t, 2H, OCH2, J = 6.4), 2.34 (t, 2H, CH2COOEt, J = 7.2), 2.31 (t, 2H, CH2-COOEt, J = 7.2), 1.90–1.78 (m, 12H, CH2), 1.68 (m, 4H, CH2), 1.60–1.47 (m, 12H, CH2), 1.37 (m, 16H, CH2), 1.258 (t, 6H, CH3, J = 7.2), 1.255 (t, 6H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 173.9, 173.8 (Cq, C=O), 167.8 (Cq, N=C–S), 159.39, 159.33 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.3 (Ct), 129.6 (Cq), 127.9 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.44, 115.39, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.7 (C(C), 69.8, 69.7, 68.0, 67.8 (OCH2), 60.43, 60.38 (COOCH2CH3), 34.4, 34.1 (CH2COOEt), 31.8, 29.5, 29.2, 29.0, 25.9, 25.8, 25.0, 24.8, 22.83, 22.81, 21.7 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C87H104N2O10S: C 76.28, H 7.65, N 2.05, S 2.34; Found: C 76.12, H 7.55, N 2.11, S 2.18; FD MS: m/z [%]: 1368.6 (88, [M+1]+); 1367.8 (100, M+).

2-{4-[4-{4-[7-(Ethoxycarbonyl)heptyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-{4-[4-{4-[6-(ethoxycarbonyl)hexyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (2e) Hexane/EtOAc = 7/1 (Rf = 0.1), yellow solid; yield 100 mg (68%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.13 (q, 4H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.970 (t, 2H, OCH2, J = 6.4), 3.968 (t, 2H, OCH2, J = 6.4), 2.32 (t, 2H, CH2COOEt, J = 7.6), 2.30 (t, 2H, CH2COOEt, J = 7.6), 1.90–1.76 (m, 12H, CH2), 1.60–1.32 (m, 34H, CH2), 1.26 (t, 6H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.0, 173.9 (Cq, C=O), 167.8 (Cq, N=C–S), 159.41, 159.38 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.3 (Ct), 129.6 (Cq), 127.9 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.39, 115.36, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.7 (C≡C), 69.8, 69.7, 68.1, 68.0 (OCH2), 60.37, 60.35 (COOCH2CH3), 34.5, 34.4 (CH2COOEt), 31.8, 29.5, 29.3, 29.2, 29.0, 28.7, 26.0, 25.9, 25.02, 25.00, 22.82, 22.80 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C89H108N2O10S: C 76.47, H 7.79, N 2.00, S 2.29; Found: C 76.17, H 7.73, N 2.18, S 2.29; FD MS: m/z [%]: 1396.5 (100, [M+1]+); 1395.5 (94, M+).

2-{4-[4-{4-[10-(Ethoxycarbonyl)decyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-{4-[4-{4-[4-(ethoxycarbonyl)butoxy]phenylethynyl}-2,5-bis-(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (2f) Hexane/EtOAc = 7/1 (Rf = 0.1), yellow solid; yield 100 mg (67%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.64 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.14 (q, 2H, COOCH2CH3, J = 7.2), 4.12 (q, 2H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.97 (m, 4H, OCH2), 2.39 (t, 2H, CH2COOEt, J = 7.2), 2.29 (t, 2H, CH2COOEt, J = 7.2), 1.90–1.74 (m, 14H, CH2), 1.66–1.50 (m, 12H, CH2), 1.50–1.30 (m, 26H, CH2), 1.26 (t, 3H, CH3, J = 7.2), 1.25 (t, 3H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.0, 173.6 (Cq, C=O), 167.8 (Cq, N=C–S), 159.4, 159.2 (Cq, C–OCH2), 154.0, 153.5 (Cq, C–OC6H13), 133.2, 132.3 (Ct), 129.6 (Cq), 127.9 (Ct), 126.7 (Cq), 117.0, 116.8 (Ct), 115.5, 115.3, 115.23, 115.18 (Cq), 114.63, 114.60 (Ct), 112.89, 112.86 (Cq), 95.6, 95.5, 94.1, 89.2, 84.7, 84.6 (C(C), 69.8, 69.7, 68.2, 67.6 (OCH2), 60.5, 60.3 (COOCH2CH3), 34.5, 34.1 (CH2COOEt), 31.8, 29.6, 29.51, 29.50, 29.46, 29.44, 29.38, 29.33, 29.27, 28.7, 26.1, 25.9, 25.1, 22.81, 22.79, 21.8 (CH2), 14.4, 14.2 (CH3); EA: Calc. for C90H110N2O10S: C 76.56, H 7.85, N 1.98, S 2.27; Found: C 76.38, H 7.65, N 2.36, S 2.08; FD MS: m/z [%]: 1411.3 (97, M+); 1410.3 (100).

2-{4-[4-{4-[10-(Ethoxycarbonyl)decyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-5-{4-[4-{4-[7-(ethoxycarbonyl)heptyloxy]phenylethynyl}-2,5-bis(hexyloxy)phenyl]ethynylphenyl}-1,3,4-thiadiazole (2g) Hexane/EtOAc = 10/1 (Rf = 0.1), yellow solid; yield 88 mg (64%). 1H NMR (400 MHz, CDCl3): ( = 8.01 (4H, AA’BB’), 7.65 (4H, AA’BB’), 7.46 (4H, AA’BB’), 7.02 (s, 2H), 7.01 (s, 2H), 6.86 (4H, AA’BB’), 4.13 (q, 2H, COOCH2CH3, J = 7.2), 4.12 (q, 2H, COOCH2CH3, J = 7.2), 4.05 (t, 4H, OCH2, J = 6.4), 4.04 (t, 4H, OCH2, J = 6.4), 3.97 (t, 4H, OCH2, J = 6.4), 2.30 (t, 2H, CH2COOEt, J = 7.2), 2.29 (t, 2H, CH2COOEt, J = 7.2), 1.90–1.74 (m, 12H, CH2), 1.68–1.28 (m, 46H, CH2), 1.258 (t, 3H, CH3, J = 7.2), 1.255 (t, 3H, CH3, J = 7.2), 0.91 (t, 6H, CH3, J = 7.2), 0.90 (t, 6H, CH3, J = 7.2); 13C NMR (100 MHz, CDCl3): δ = 174.1, 174.0 (Cq, C=O), 167.8 (Cq, N=C–S), 159.4 (Cq, C–OCH2), 154.0, 153.6 (Cq, C–OC6H13), 133.2, 132.4 (Ct), 129.6 (Cq), 128.0 (Ct), 126.7 (Cq), 117.2, 116.8 (Ct), 115.4, 115.2 (Cq), 114.6 (Ct), 112.9 (Cq), 95.6, 94.1, 89.2, 84.7 (C≡C), 69.8, 69.7, 68.2, 68.1 (OCH2), 60.36, 60.32 (COOCH2CH3), 34.54, 34.48 (CH2COOEt), 31.8, 29.63, 29.50, 29.47, 29.45, 29.40, 29.34, 29.28, 29.19, 26.2, 26.0, 25.9, 25.12, 25.03, 22.82, 22.81 (CH2), 14.4, 14.2 (CH3). EA: Calc. for C93H116N2O10S: C 76.82, H 8.04, N 1.93, S 2.21; Found: C 76.62, H 8.09, N 1.89, S 2.03. FD MS: m/z [%]: 1453.2 (100, M+).

Reference

- Wadsworth, H. J.; Widdowson, D. A.; Wilson, E.; Carroll, M. A. Radical trap in fluoridation of iodonium salt. WO 2005/061415 A1, July 7, 2005.